AEROSPACE TEST SPECIMEN STANDARDS

Reference Document — Dimensional Requirements, Applicable Standards & Test Purpose

Prepared for Internal Reference Use  |  Corrosion, Fatigue & Mechanical Test Specimens

1. SCOPE & PURPOSE

This document consolidates dimensional requirements, material specifications, and test purpose definitions for aerospace corrosion and mechanical test specimens. It serves as a reference for incoming inspection, manufacturing scope review, RFQ preparation, and material traceability activities.

Standards covered include ASTM, SAE AMS, and European aerospace (EN) test specimen specifications applicable to corrosion testing, hydrogen embrittlement evaluation, fatigue life testing, and thermal spray coating assessment.

2. SALT SPRAY TEST SPECIMENS

2.1 ASTM B117 — Neutral Salt Spray (NSS)

Standard: ASTM B117 — Standard Practice for Operating Salt Spray (Fog) Apparatus

Purpose: Provides a controlled, accelerated corrosive environment to evaluate the relative corrosion resistance of metals, coated metals, and surface treatments. Primarily used for comparative analysis and quality control — not for predicting absolute service life. First published in 1939; internationally recognized across aerospace, automotive, marine, and defence sectors.

Test Environment: 5% sodium chloride (NaCl) solution at 35°C ± 2°C. Fog collection rate: 1.0–2.0 mL/hr per 80 cm². pH of collected solution: 6.5–7.2.

Specimen Requirements

ASTM B117 does not mandate specific specimen dimensions — dimensions are defined by the product specification or customer requirement. Standard practice panels used across the industry:

| Parameter | Value / Specification |
| --- | --- |
| Standard Panel Size | 3" × 5" × 0.032" (75 × 125 × 0.8 mm) — NSS calibration panel |
| Common Test Panel Size | 3" × 6" (75 × 150 mm) or 4" × 6" (100 × 150 mm) |
| Maximum Thickness | 0.040" (1.0 mm) for standard flat panels |
| Calibration Panel Material | 1008 Cold-Rolled Mild Steel |
| Specimen Orientation | 15°–30° from vertical during exposure |
| Surface Preparation | Degrease, clean; scribe marks applied if required by spec |
| Common Test Durations | 96 hr, 168 hr, 240 hr, 500 hr, 1000 hr (per product spec) |
| Industries | Aerospace, Automotive, Marine, Defence, Electronics |

Notes

•  Specimens must not contact each other during exposure — fog distribution must not be impeded.

•  ASTM B117 does not define pass/fail criteria — acceptance criteria are defined by the governing product specification.

•  Related standards: ASTM G85 (cyclic corrosion), ISO 9227 (international equivalent), MIL-STD-810 (military reference).

2.2 ASTM B368 — Copper-Accelerated Acetic Acid Salt Spray (CASS Test)

Standard: ASTM B368 — Standard Test Method for Copper-Accelerated Acetic Acid-Salt Spray (Fog) Testing

Purpose: A significantly more aggressive accelerated corrosion test than neutral salt spray (ASTM B117). Designed to rapidly evaluate the durability of decorative and functional metallic coatings. Used for copper/nickel/chromium (Cu/Ni/Cr) coatings, anodized aluminum, and die castings. Widely applied in aerospace, automotive, and electronics quality control.

Test Environment: Sodium chloride solution acidified with acetic acid and copper chloride. Test temperature: 49°C ± 1°C. pH: 3.1–3.3.

Specimen Requirements

| Parameter | Value / Specification |
| --- | --- |
| Specimen Type | Decorative coated panels — Ni/Cr, Cu/Ni/Cr, anodized aluminum |
| Calibration Panel Size | 7.5 × 10 cm (~3" × 4"), ~0.09 cm thick |
| Calibration Panel Material | Nickel-plated steel (specific nickel panels required to verify chamber corrosivity) |
| Surface Condition | Coating must be free of pores, cracks, and blistering before test |
| Industries | Aerospace, Automotive, Electronics |

2.3 ASTM F1110 — Sandwich Corrosion Test (Boeing Sandwich Test)

Standard: ASTM F1110 — Standard Test Method for Sandwich Corrosion Test

Purpose: Evaluates the corrosivity of aircraft maintenance chemicals on aluminum alloy structural materials. Also known as the Boeing Sandwich Test. Simulates the entrapment of maintenance fluids between faying surfaces, representative of real aircraft structural joint conditions.

Applicable Materials: Primarily 2024-T3 (bare or clad) and 7075-T6 (bare or clad) aluminum alloys — the primary structural alloys in commercial and military aircraft.

Specimen Requirements

| Parameter | Value / Specification |
| --- | --- |
| Coupon Dimensions | 2" × 4" × 0.062" (50 × 100 × 1.57 mm) |
| Material | 2024-T3 (bare or clad) or 7075-T6 (bare or clad) per AMS 2024 / AMS 7075 |
| Specimen Quantity | Minimum 3 coupons per test chemical |
| Surface Condition | As-received or chemically treated per test requirements |
| Test Configuration | Chemical solution sandwiched between two coupons with filter paper |
| Evaluation Criteria | Mass loss (mg/cm²), surface corrosion rating, pitting depth |
| Industries | Aerospace, Defence — Aircraft Maintenance Chemical Qualification |

3. ATMOSPHERIC CORROSION TEST SPECIMENS

3.1 ASTM G50 — Atmospheric Corrosion Testing

Standard: ASTM G50 — Standard Practice for Conducting Atmospheric Corrosion Tests on Metals

Purpose: Defines procedures for exposing metals and alloys to outdoor environments to evaluate long-term corrosion resistance or the corrosivity of specific geographic locations. Used for material selection, alloy development, and coating system evaluation in actual service conditions.

Specimen Requirements

| Parameter | Value / Specification |
| --- | --- |
| Recommended Panel Size | 4" × 6" (100 × 150 mm) — standard |
| Alternative Panel Size | 4" × 8" (100 × 200 mm) |
| Minimum Thickness | 0.030" (0.75 mm) — for structural rigidity |
| Standard Thickness | 0.032" (0.81 mm) — most common |
| Maximum Thickness | 0.250" (6.35 mm) with standard insulators; thicker specimens require special deep-throated insulators |
| Mounting | Non-metallic insulators at corners to prevent galvanic interference |
| Exposure Angle | 45° to horizontal (in northern hemisphere, facing south) |
| Evaluation | Mass loss (g/m²), corrosion rate (µm/year), visual rating |

3.2 ASTM G69 — Corrosion Potential of Aluminum Alloys

Standard: ASTM G69 — Standard Test Method for Measurement of Corrosion Potentials of Aluminum Alloys

Purpose: Measures the open-circuit (rest) corrosion potential of aluminum alloys in a standard sodium chloride + hydrogen peroxide solution. Used to characterize the electrochemical behavior and metallurgical condition of aluminum alloys — important for identifying susceptibility to intergranular corrosion and galvanic coupling risk.

Applicable Materials: All wrought and cast aluminum alloys — particularly 2024, 7075, 6061, 7050, and clad variants.

Specimen Requirements

| Parameter | Value / Specification |
| --- | --- |
| Recommended Size | 15 mm × 100 mm (0.60" × 3.9") |
| Standard Thickness | ~3 mm (1/8") for bulk material specimens |
| Surface Finish | 600-grit SiC paper finish; cleaned with acetone before testing |
| Test Solution | 53 g/L NaCl + 3 g/L H₂O₂ at 25°C ± 3°C |
| Reference Electrode | Saturated Calomel Electrode (SCE) |
| Measurement | Open-circuit potential (mV vs. SCE) after 10-min stabilization |
| Applicable Alloys | 2024-T3, 7075-T6, 6061-T6, 7050-T7451 and clad variants |

4. STAINLESS STEEL & SPECIALTY ALLOY CORROSION SPECIMENS

4.1 ASTM G48 — Pitting and Crevice Corrosion (Stainless Steel & Ni-Alloys)

Standard: ASTM G48 — Standard Test Methods for Pitting and Crevice Corrosion Resistance of Stainless Steels and Related Alloys

Purpose: Evaluates resistance of stainless steels and nickel-based alloys to pitting and crevice corrosion using ferric chloride (FeCl₃) solution — simulates aggressive oxidizing chloride environments. Critical for materials in oil & gas, marine, chemical processing, and aerospace fluid systems.

Test Methods: Method A (pitting corrosion), Method B (crevice corrosion), Methods C–F (critical temperature variants).

Specimen Requirements

| Parameter | Value / Specification |
| --- | --- |
| Recommended Size | 25 × 50 mm (1" × 2") flat rectangular plate |
| Length Range | 25–80 mm (up to 80 mm for weldment testing) |
| Thickness | Matches original material thickness (representative of actual application) |
| Surface Finish | 120-grit or finer; edges chamfered or rounded to remove burrs |
| Minimum Solution Ratio | 5 mL FeCl₃ solution per cm² of specimen surface area |
| Test Solution | 6% FeCl₃·6H₂O (ferric chloride hexahydrate) in distilled water |
| Evaluation | Mass loss (mg/cm²), pit depth, pit density, visual surface rating |
| Applicable Materials | 300-series CRES, 400-series CRES, Duplex SS, Ni-alloys (625, 825) |

4.2 SAE AMS-C-26074 §4.5.5 — Nickel Plating Corrosion Test Panels

Standard: SAE AMS-C-26074 — Electroless Nickel Plating Requirements

Purpose: Specifies corrosion test specimens used to verify electroless nickel plating quality when actual production parts are unsuitable for testing due to shape, size, or form. Test specimens undergo ASTM B117 neutral salt spray testing as part of coating qualification and periodic quality checks.

Specimen Requirements

| Parameter | Value / Specification |
| --- | --- |
| Specimen Dimensions | 4" × 6" × 0.040" (101.6 × 152.4 × 1.0 mm) |
| Material | Same base metal as the plated production parts |
| Surface Preparation | Same pre-treatment sequence as production parts (clean, activate, plate) |
| Test Method | ASTM B117 Neutral Salt Spray — per specification test duration |
| Acceptance | No corrosion products, blistering, or loss of adhesion per AMS-C-26074 requirements |

4.3 ASTM F482 — Corrosiveness of Aircraft Maintenance Chemicals (Immersion)

Standard: ASTM F482 — Standard Practice for Evaluating Corrosiveness of Aircraft Maintenance Chemicals on Metals (Immersion)

Purpose: Evaluates how aircraft cleaning agents, de-icers, hydraulic fluids, and other maintenance chemicals affect various aircraft-grade alloys through total immersion. Complements ASTM F1110 sandwich test and is used for maintenance chemical qualification on aerospace programs.

Specimen Requirements

| Parameter | Value / Specification |
| --- | --- |
| Specimen Dimensions | 50.8 × 25.4 × 1.6 mm (2" × 1" × 0.063") |
| Mounting Hole | 3.2 mm (0.125") diameter hole at one end for suspension |
| Total Surface Area | ~28.2 cm² (4.4 in²) per specimen |
| Specimen Quantity | 5 per alloy (4 immersed + 1 control for visual comparison) |
| Applicable Alloys | 2024-T3, 7075-T6, 6061-T6, 4130 steel, titanium Ti-6Al-4V, CRES 301/304 |
| Evaluation | Mass loss (mg/cm²), tensile strength retention (%), visual surface condition |

5. THERMAL SPRAY COATING ADHESION SPECIMENS

5.1 ASTM C633 — Adhesion/Cohesion of Thermal Spray Coatings

Standard: ASTM C633 — Standard Test Method for Adhesion or Cohesion Strength of Thermal Spray Coatings

Purpose: Determines the adhesion strength between a thermal spray coating and its substrate, or the internal cohesion strength of the coating itself. Critical quality control and process development tool for plasma arc, combustion flame, and HVOF (High-Velocity Oxygen Fuel) spray processes used in aerospace component repair and surface engineering.

Specimen (Fixture) Requirements

| Parameter | Value / Specification |
| --- | --- |
| Geometry | Solid cylinder — coated substrate fixture + loading fixture |
| Diameter | 1.0" (25.4 mm) nominal; tolerance 0.9"–1.0" (23–25 mm) |
| Diameter Match | Both fixtures must match within 0.5% of each other |
| Minimum Length | 1.5" (38 mm) per fixture |
| Substrate Material | Same metal as actual application; default SAE 1018 or 1020 steel if unspecified |
| Surface Preparation | Grit-blast substrate before coating to achieve required anchor profile (Ra) |
| Minimum Coating Thickness | 0.015" (0.38 mm) — prevents adhesive from penetrating coating pores |
| Adhesive | High-strength structural adhesive (e.g., FM-1000 or equivalent) — cure per adhesive spec |
| Test Method | Uniaxial tensile pull test at controlled crosshead speed |
| Failure Mode Recording | Adhesive, cohesive, or mixed failure; location within coating must be recorded |

•  Common thermal spray processes: Plasma Arc Spray, Combustion Flame Spray, HVOF, Cold Spray.

•  HVOF coatings typically achieve adhesion values >70 MPa; plasma spray 20–50 MPa depending on material and substrate.

•  Used for Nadcap-accredited thermal spray process qualification and periodic quality audits.

6. HYDROGEN EMBRITTLEMENT TEST SPECIMENS

6.1 ASTM F519 — Mechanical Hydrogen Embrittlement Evaluation

Standard: ASTM F519 — Standard Test Method for Mechanical Hydrogen Embrittlement Evaluation of Plating/Coating Processes and Service Environments

Purpose: Evaluates whether electroplating, chemical coating, or pre-treatment cleaning processes introduce dangerous levels of hydrogen into high-strength steels — causing delayed, catastrophic brittle fracture. Managed by ASTM Subcommittee F07.04. Critical standard for aerospace fastener manufacturing, electroplating process qualification, and Nadcap accreditation of plating processes.

Primary Applications:

•  
      Process Qualification: Confirms that a specific plating or chemical processing line will not cause high-strength steel parts to embrittle and fracture under sustained load.

•  
      Periodic Quality Assurance: Regular production monitoring for continuous electroplating lines supplying aerospace hardware.

•  
      Service Environment Verification: Evaluates risk from maintenance chemicals (cleaners, de-icers, paint strippers) that contact high-strength steel parts in service.

•  
      Bake Relief Verification: Confirms that post-plate hydrogen embrittlement relief baking (per AMS 2759/9) has been effective.

Required Material: High-strength steel — minimum 220 ksi (1517 MPa) UTS. Typical alloys: 4340, 300M, H-11 (AMS 6487), 17-4 PH (H900 condition). Hardness: typically 54–56 HRC for Type 1a specimens.

Type 1a.1 Specimen — Standard Notched Tensile Bar

| Parameter | Value / Specification |
| --- | --- |
| Total Length (L) | 50.8 mm (~2.000") |
| Major (Outer) Diameter (D) | 9.0 mm (~0.375") |
| Minor (Notch Root) Diameter (d) | 6.35 mm ± 0.05 mm (0.250" ± 0.002") |
| Notch Angle | 60° inclusive V-notch |
| Notch Root Radius (R) | 0.25 mm ± 0.013 mm (0.010" ± 0.0005") |
| Grip / Thread Ends | M12 metric threads or 3/8"-24 UNF threads |
| Surface Finish at Notch | ≤ 32 µin Ra (0.8 µm Ra) — machined and ground to spec |
| Load Application | Sustained tensile load at 75% of notch fracture strength for minimum 200 hours |
| Failure Criterion | Specimen fractures within 200 hr = hydrogen embrittlement present |
| Pass Criterion | No fracture after 200 hr sustained load = process acceptable |

Type 1a.2 Specimen — Large Notched Tensile Bar (Button Head)

| Parameter | Value / Specification |
| --- | --- |
| Total Length | 152.4 mm (6.000") |
| Major (Outer) Body Diameter | 14.30 mm (~0.563") |
| Minor (Notch Root) Diameter (d) | 9.04 mm ± 0.05 mm (0.356" ± 0.002") |
| Notch Angle | 60° standard; 90° ± 1° alternate (requires prior engineering approval) |
| Notch Root Radius | 0.38 mm ± 0.025 mm (0.015" ± 0.001") |
| Grip Ends | Button-head flanged shoulders — 22.22 mm (0.875") diameter |
| Grip Type | Split-collar tensile testing grips |
| Surface Finish at Notch | ≤ 32 µin Ra (0.8 µm Ra) |
| Load Application | Sustained tensile load per specification — minimum 200 hours |
| Typical Application | Larger fastener and structural component coating process qualification |

Manufacturing & Heat Treatment Requirements

•  All F519 specimens must be machined from bar stock meeting minimum UTS and hardness requirements before plating.

•  Notch geometry is the critical feature — notch root radius tolerance is ±0.013 mm (Type 1a.1) — requires precision CNC turning and grinding.

•  Surface finish at notch root must be ≤ 32 µin Ra — typically achieved by finish grinding after turning.

•  
      Pre-plate condition: Specimens are heat treated to final hardness (typically 54–56 HRC for 4340 steel) BEFORE machining of notch root — sequence is critical.

•  
      Post-plate bake: AMS 2759/9 requires hydrogen embrittlement relief bake at 190°C ± 14°C for minimum 8 hours within 4 hours of plating — F519 test specimens verify bake effectiveness.

•  Dimensional inspection per AS9102 FAI requirements recommended before sustained load testing.

7. FATIGUE TEST SPECIMENS

7.1 EN 6072 — Constant Amplitude Fatigue Testing (Aerospace Series)

Standard: EN 6072:2010 — Aerospace Series — Metallic Materials — Test Methods — Constant Amplitude Fatigue Testing

Purpose: Defines the method to determine constant amplitude fatigue data of metallic materials and generate S-N (Wöhler) curves — plotting stress amplitude against cycles to failure. The standard ensures that aerospace manufacturers worldwide use identical specimen dimensions, machining tolerances, and test controls to produce comparable, repeatable materials data for structural design.

Governing Body: CEN (European Committee for Standardization) — adopted as BS EN 6072 (UK), DIN EN 6072 (Germany), and national equivalents. Referenced by Airbus material and process specifications (AIMS series).

Specimen Configurations (per EN 6072 Annexes):

•  
      Annex A: Axial Fatigue — Cylindrical specimen (smooth, Kt = 1.0)

•  
      Annex B: Axial Fatigue — Flat specimen (Kt = 1.0)

•  
      Annex C: Axial Fatigue — Flat "T-Type" and mini "T-Type" specimen (Kt = 2.3)

•  
      Annex D: Bending Fatigue — Flat specimen

•  
      Annex E: Machining procedure recommendations

Cylindrical Specimen — Kt = 1.7 (V-Notch Configuration)

| Parameter | Value / Specification |
| --- | --- |
| Total Length (L) | 80.0 mm (standard frame-to-grip envelope) |
| Shank / Grip Diameter (D) | 12.0 mm |
| Thread Profile | M16 × 1.0 metric — both ends (for rigid hydraulic alignment) |
| Net Diameter at Notch Root (d) | 6.0 mm |
| Stress Concentration Factor (Kt) | 1.7 (V-notch geometry) |
| Included Notch Angle | 60° symmetrical V-notch — centered along gauge length |
| Notch Root Radius (ρ) | 1.0 mm (critical micro-machined radius — controls Kt) |
| Surface Finish — Gauge Section | ≤ 0.4 µm Ra (longitudinal polish direction) |
| Surface Finish — Notch Root | ≤ 0.4 µm Ra — achieved by precision grinding |
| Straightness | ≤ 0.05 mm over full specimen length |
| Coaxiality | Notch root to grip axis ≤ 0.02 mm TIR |

Test Parameters

| Parameter | Value / Specification |
| --- | --- |
| Loading Mode | Constant amplitude axial (tension-compression or tension-tension) |
| Load Ratio (R) | Defined by relevant material or process standard |
| Test Frequency | ≤ 100 Hz (to avoid adiabatic heating effects in specimen gauge section) |
| Temperature | 23°C ± 5°C unless otherwise specified |
| Failure Definition | Complete fracture of specimen OR defined crack length (per agreement) |
| Run-out Definition | Typically 10⁷ cycles (defined by governing material standard) |
| Minimum Specimens per S-N Curve | Minimum 8–12 specimens recommended for statistical validity |
| Data Presentation | S-N curve (log stress vs. log cycles); Wöhler curve format |

Manufacturing Requirements for EN 6072 Specimens

•  All machining operations must be performed in the sequence defined by the process plan — heat treatment before final machining of gauge section is standard practice.

•  Final gauge and notch machining must be performed after heat treatment — heat treatment distortion must not affect final dimensional compliance.

•  Surface finish in the gauge length and notch root is critical — residual machining marks perpendicular to loading direction act as stress raisers and invalidate results.

•  All specimens from a batch must be from the same heat of material, same heat treatment lot, and same machining setup where possible.

•  Material certification (C of C) must confirm alloy, heat/lot number, temper, AMS specification, and mechanical properties before specimen fabrication.

•  Common materials: Aluminum 2024-T3, 7075-T6, 7050-T7451; Steel 4130, 4340; Titanium Ti-6Al-4V; CRES 17-4 PH.

8. QUICK REFERENCE — STANDARDS SUMMARY

| Standard | Test Type | Key Specimen Size | Primary Material | Industry |
| --- | --- | --- | --- | --- |
| ASTM B117 | Neutral Salt Spray | 75×150 mm flat panel | 1008 CRS / Per spec | Aerospace, Auto |
| ASTM B368 | CASS (Accelerated) | 7.5×10 cm Ni calibration panel | Ni-plated steel | Aerospace, Auto |
| ASTM F1110 | Sandwich Corrosion | 2"×4"×0.062" | 2024-T3, 7075-T6 Al | Aerospace |
| ASTM G50 | Atmospheric Corrosion | 4"×6"×0.032" panel | Per alloy spec | Aerospace, Marine |
| ASTM G69 | Corrosion Potential | 15×100×3 mm | Aluminum alloys | Aerospace |
| ASTM G48 | Pitting/Crevice (SS) | 25×50 mm flat plate | 300/400 CRES, Ni-alloys | Aerospace, O&G |
| AMS-C-26074 | Ni Plate Corrosion | 4"×6"×0.040" | Same as plated part | Aerospace |
| ASTM F482 | Maintenance Chemical | 50.8×25.4×1.6 mm | Al, Steel, Ti, CRES | Aerospace |
| ASTM C633 | Thermal Spray Adhesion | 1"Ø × 1.5" cylinder | SAE 1018/1020 steel | Aerospace, Defence |
| ASTM F519 Type 1a.1 | H.E. — Notch Tensile | Ø9×50.8 mm notched bar | 4340/300M HRC 54–56 | Aerospace, Defence |
| ASTM F519 Type 1a.2 | H.E. — Button Head | Ø14.3×152.4 mm notched bar | 4340/300M HRC 54–56 | Aerospace, Defence |
| EN 6072 (Kt=1.7) | Constant Amp Fatigue | Ø12×80 mm V-notch bar | Al, Steel, Ti alloys | Aerospace (Airbus) |

This document is compiled from publicly available ASTM, SAE AMS, and EN aerospace standards for internal reference use.

All proprietary company data, customer programs, part numbers, and pricing have been excluded. Standards remain the authoritative source.